## Slide 1
NAKUJA 4 SOLIDS TEAM
WEEK 2 PROGRESS REPORT

## Slide 2
THIS WEEK’S OBJECTIVES:
  Analysis and research of the previous static test
  Preparation of the tensile test workpieces
  Conducted the tensile test on the specimens.
  Developing calculations for the new casing.
  Searching for suppliers of the new casing.
  Cutting of the bulkhead material.
  Re-making of the liner.

## Slide 3
1.Results from the analysis
  Calculated working pressure was found to be equal to the simulated motor pressure.
  The liner acted as an insulating layer and ablative layer where pyrolysis occurred.

## Slide 4
2.Preparation of the tensile test work pieces
Using hacksaws,square files and round file a work piece was made from the aluminium casing according to the ASTM B557M Standard.
Fig 1: Dimensions of work piece with standards

## Slide 5
Photo of the activity.
Fig 3. Workpieces after activity
Fig 2. Workpiece preparation

## Slide 6
3.Tensile testing
The specimen were tested using a Shimadzu universal tensile testing machine.
The method was customised within the Trapeziumx software and the batch number specified. The specimen was loaded onto the jaws of the machine and loading began.
Fig 4. Tensile test setup
Fig 5. Workpiece in machine

## Slide 7
Results of the tensile test

## Slide 8
Excel analysis of the results
Sample 1 stress-strain curve
Sample 2 stress-strain curve

## Slide 9
Mechanical properties from the supplier

## Slide 10
Conclusion of the test
From the tensile test, it is evident that the Yield stress from the supplier was concurrent with yield stress of the test. The same is true for the Ultimate tensile stress

## Slide 11
Material properties of different Al alloys
Al 6063 T5
Al 6061 T6

## Slide 12
4.Calculation of the casing
Fig 12. Casing calculations for AL 6063 T5
Fig 12. Casing calculations for AL 6061 T6

## Slide 13
5.Suppliers from the internet
Fig 14&15. Alibaba supplier

## Slide 14
6. Cutting of the bulkhead to specific size.
Fig 16. Bulkhead material cut to dimension

## Slide 15
Re-making of the Liner according to the new casing dimensions
Fig 16. Liner made to 94mm dimension

## Slide 16
NEXT WEEK’S OBJECTIVES
  Simulating of the new casing performance in Ansys
  Machining of the bulkheads to be used in the hydrostatic test (consult on how to conduct our own pressure test during hot fires - piping system connection)
  Conducting the hydrostatic test
  Obtaining Sorbitol and Potassium Nitrate
  Cooking of the grains

## Slide 17
THANK YOU
N4 SOLIDS TEAM